Process Protocol <device xyz>

Subtitle

| Protocol No.: | Wafer | Okmetic | 771/40393 | Qty. | 50 | prime | 100 mm ,100> |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Substrate: 390 m n/P 3-5 Ohmcm Surfaces: polished/polished |  |  |  |  |  |

| Nr. Process step | Substep |  |  | Parameter |  |  |  |  |  | Value |  |  | Comment Date/signature |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1.0 Initial cleaning | H2SO4/H2O2 |  |  | Temperature [C]: Time [min]: |  |  |  |  |  | 120 7 |  |  |  |  |  |  |
|  | DI-water rinse |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Rinser Dryer |  |  | 99 s /111 s / 222 s |  |  |  |  |  |  |  |  |  |  |  |  |
| 2. Oxidation | Oxidation Wet 500 nm  2 nm |  |  | Process name: Process temperature [C]: Process time [C]: Tube no.: batch no.: wafer separation during ox.: |  |  |  |  |  | FOX1000 1000 1h 26 m 1B4 |  |  |  |  |  |  |
|  | Measurement Film thickness |  |  | n (Ellipsometer): Program (MPV): |  |  |  |  |  | 45 |  |  |  |  |  |  |
|  |  | Left |  |  |  | Center left |  |  | Center right |  |  |  |  | right |  |  |
|  |  | W.No. L: | W.No. C: |  | W.No. R: | W.No. L: | W.No. C: | W.No. R: | W.No. L: |  | W.No. C: | W.No. R: |  | W.No. L: | W.No. C: | W.No. R: |
|  | d [nm]  [nm] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Min: Max: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3.0 Lithography | Spin on resist |  |  | Resist: Process name: Rpm 1[min-1]: Time [s]: Rpm 2[min-1]: Time[s]: |  |  |  |  |  | AZ 1514 |  |  |  |  |  |  |
|  | Pre-bake |  |  | Temperature [C]: Time [min]: |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Exposure MA1006 Mask: SiC-Struct. Alignment Mark: 1 |  |  | Program: Exposure time [s]: Power (405 nm) [W]: [mW/cm2]: |  |  |  |  |  | 3 8 250 20 |  |  |  |  |  |  |
|  | Develop |  |  | Manually, developer bath Developer: Time [min]: |  |  |  |  |  | AZ 1 m 30s |  |  |  |  |  |  |
|  | Inspection |  |  | Structure width mask: (e.g. alignment mark) Structure width resist: (delta> 0.3 m -> new Lithography) |  |  |  |  |  | 10 m |  |  |  |  |  |  |
| 4.0 Pattern oxide | RIE Oxide etch (Vacutec) |  |  | Process name: Process time: SF6 flow [sccm]: Pressure [mbar]: Power [W]: |  |  |  |  |  | Nitride etch 4 m 20 150 150 |  |  |  |  |  |  |
|  | Inspection: |  |  | Etch rate oxide: |  |  |  |  |  |  |  |  |  |  |  |  |